## Slide 1
The Study of Material and Electrical Properties of Ag-Cu alloy thin films applied on RRAM
Different composition of AgCu alloy
 | Ag | Cu
specimen1 | 42 | 58
specimen2 | 49 | 51
specimen3 | (25) | (75)
Ag42Cu58
Ag49Cu51
Ag(111)
Cu(111)
Ag(111)
Cu(111)
XRD
XPS
Sample
V
AgCu
SiO2
TiN
TiN
AgCu
SiO2
Switching layer
Electrical results
Ag49Cu51 & Ag42Cu58 &Ag25Cu75
C.C. 5mA
Preliminary summary
1.The more Cu in composition, the more stable in I-V sweep.
2.The coexistence of unipolar and bipolar I-V sweep appears in all three composition.
Ag42Cu58
Ag49Cu51
(Ag25Cu75)